Technical Data

|  |  | PFA |  |  |
| --- | --- | --- | --- | --- |
| Ø Outside | Ø Inner | Wall Thickness | Working Pressure | Brust Pressure |
| Inch | mm | mm | bar | bar |
| 1/2“ | 9,50 | 1,60 | 7 | 25 |
| 3/4" | 15,80 | 1,60 | 4,5 | 10 |

| Bending radius | 1/2" | 15,00 |
| --- | --- | --- |
| mm | 3/4" | 20,00 |

Co-extruded Corrugated tubing with antistatic outer layer enable ultra-flexible handling of the QC-System. Ideal for vertical and horizontal installation of the suction line.

Properties:

- More stable compared to usual corrugated PFA tubing due to inwards corrugation

- Conductive Flare connections on both ends tube

- 10cm-long straight hose ends on both sides so that the QC Dispense Head can easily be connected with the flare connecting system

Technical Specifications

| Material | - Inside virgin PFA - Outside antistatic PFA |
| --- | --- |
| Nominal widths | - 1/2" - 3/4“ *more available on request |
| Max Length | - 1/2" up to 4,5 meters - 3/4" up to 6 meters |
| Working Temperature | - Up to 60°C |
| End Connections | - 10 cm-long straight hose ends on both sides |

*incl. Flare nuts CD/PVDF on both sides

Standard Versions

| Size in Inch | Usability length in mm* | Item-no. |
| --- | --- | --- |
| 1/2" | 1000 | R12S121-CD-CT-1-230-FL |
| 1/2" | 2000 | R12S121-CD-CT-2-230-FL |
| 3/4“ | 2000 | R12S122-CD-CT-2-230-FL |
| 3/4" | 3000 | R12S122-CD-CT-3-230-FL |